## Slide 1: Carbon-neutral Energy and Nutrient Recovery from Solid Manures
Wayne Yuan, Dwi Cahyani
Dept. of Bio. and Ag. Engineering
NC State University

## Slide 2: The Challenge: GHG, Waste, Fertilizer Shortage
Waste management
Greenhouse gas emissions
Global CO2e emissions. Obtained from Statista.
Global waste composition. Obtained from Sustainability.

## Slide 3: Project Purpose
Project Goals and Objectives
Manure collection, separation, drying, and characterization
Syngas production from TLUD gasification of dried solid manure
Nutrient analysis of ash-biochar blends from TLUD gasification

## Slide 4: Biochar
What is it?
Carbon-rich material produced from organic waste or biomass
Produced via thermochemical conversion
What it is used for?
Enhances soil fertility
Stable form of long-term carbon storage
Precursor for high-value products
Potential applications of biochar. (Biochar Industry, 2023)
Notes: heating biomass in a low-oxygen environment

## Slide 5: Market of Biochar
Market Analysis Report 2023
Biochar Market Size, Share and Growth Analysis Report (Grand View Research Biochar, 2023)
$541.8M
$1.35B
Notes: Historical Range: 2018-2022
Forecast Period: 2024 - 2030
Since the process does not yield stable biochar that can be used in agricultural applications,
Increasing product consumption in producing organic food and its ability to enhance soil fertility & plant growth are expected to be key factors driving market growth

## Slide 6: Manure sourcing and processing
Manure type | Farm/Source
Poultry | Pray to Lay Poultry, LLC 4591 N Nc Highway Seven Springs, NC 28578
Dairy | Kooba Dairy Inc 1719 Penny Tew Mill RD, Roseboro, NC 28382
Swine | Montauk Energy 1362 Blind Bridge Road Duplin County, NC
Woodchips | Veneer Technologies, Newport, NC
Table 1. Farm/Source of Manure
Figure 1. Manure drying process (A), wet (left) and dry (right) dairy manure (B).
A
B

## Slide 7: Animal Manure Pretreatment
Animal waste
Lake Wheeler Field Laboratories
Dried Manure
High Moisture Content
Layer Poultry Litter = 75%
Dairy Manure = 87%
(ASABE Standard)
Belt Dryer, 24+ hr
Lower Moisture Content (< 30%)

## Slide 8: Wood Veneer Waste Pretreatment
Non-uniform particles sizes
Reduces wood chips to uniform size
Uniform Particle Size
Starting Material
Mill
Ending material

## Slide 9
Wood Veneer Waste
Dried Dairy manure
Dried Poultry litter
Dried Swine manure
Raw
Biomass
Feedstock

## Slide 10: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Volume: .012 m^3

## Slide 11: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Pressure: 50-60 psi

## Slide 12: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Adjust Airflow

## Slide 13: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Add feed,
Ignite with torch

## Slide 14: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Thermocouples track temperature with datalogger

## Slide 15: Top Lit Updraft (TLUD) Gasification Unit
James, A. M., Yuan, W., Boyette, M. D., Wang, D., & Kumae, A. (2016). Characterization of Biochar from Rice Hulls and Woodchips Produced in a Top-Lit Updraft Biomass Gasifier . 2016 American Society of Agricultural and Biological Engineers, 59(3).
Capture Syngas

## Slide 16
Biochar Wood Vaneer
Biochar Dairy manure
Biochar Poultry litter
Biochar Swine manure
Biochars
produced

## Slide 17: Syngas compositions
Syngas composition
The chemical composition of syngas was measured by Gas
Chromatography, SRI 8610 with TCD and Argon carrier gas.
Syngas was captured using 10 L Tedlar bag.
Figure 4. Syngas of Dairy Manure

## Slide 18
Biomass | Airflow | Feedstock Moisture content (%) | Average Biochar Yield (%) | Max Temperature (Celcius)
Wood Veneer | 10 | 10.2 | 10.07 | 
Wood Veneer | 20 | 10.04 | 11.88 | 
Dairy | 10 | 14.58 | 19.37 | 
Dairy | 15 | - | 26.94 | 
Poultry | 10 | 16.33 | 31.18 | 
Swine | 10 | - | 22.97 | 
Average Biochar yield, Moisture content and Max gasifier Temperature.

## Slide 19: Acknowledgement
Dr. Mahmoud Sharara
Mr. Chris Hopkins
NCSU Animal and Poultry Waste Processing Facility
NCDA&CS for funding support
Veneer Technologies

## Slide 20
Thank you!